SUPPLEMENTAL SPECIFICATION NO. 4

F-162, Chain Link Fences

This Supplemental Specification amends the provisions of the Standard Specifications for Airport Construction, 1998 Edition, and shall be considered to be a part of those Standard Specifications, superseding any conflicting provisions in the Standard Specifications applicable to work under the Contract.

162-2.3  POSTS, RAILS AND BRACES.  Delete the entire section and insert the following in its place:

Posts, rails, and braces furnished for use in conjunction with aluminum-coated steel fabric shall be of zinc-coated steel, zinc/polymer-coated steel, zinc-5% aluminum mischmetal alloy coated steel framework, or composite posts.

Line posts, rails, and braces shall be galvanized steel pipe or zinc/polymer-coated steel pipe structural shapes, roll formed or composite posts conforming to the following:

Galvanized steel pipe shall conform to the requirements of ASTM F 1083.

Zinc/polymer-coated steel pipe shall conform to the requirements of ASTM A 569 or ASTM A 446,Grade D.  External coating shall be in accordance with ASTM F 1043, Type B. Internal coating shall be in accordance with ASTM F 1043, Type B or D.

The steel used in all structural shapes shall conform to the requirements of ASTM A 572, Grade 45, and shall be galvanized in accordance with the requirements of ASTM F 1043, Type A.

Roll-formed sections shall be fabricated from material meeting the requirements of ASTM A 570, Grade 45, and shall be galvanized in accordance with the requirements of ASTM F 1043, Type A, or coated with zinc-5% aluminum-mischmetal alloy in accordance with ASTM F 1043, Type C.

Composite posts shall conform to the strength requirements of ASTM F 1043. The strength loss of composite posts shall not exceed 10 percent when subjected to 3,600 hours of exposure to light and water in accordance with ASTM G 23, ASTM G 26, and ASTM G-53.

Post, rails, and braces, with the exception of galvanized steel (Schedule 40 weight) or aluminum alloy (Schedule 40 weight) which conform to the requirements of ASTM F 1083, shall demonstrate the ability to withstand testing in salt spray in accordance with ASTM B 117 as follows:

External: 1,000 hours with a maximum of 5% red rust.

Internal: 650 hours with a maximum of 5% red rust.

The dimensions of the posts, rails, and braces shall be in accordance with Tables I through VI of Fed. Spec. RR-F-191/3.

162-2.4 GATES. Delete the entire section and insert the following in its place:

Gate frames shall consist of galvanized steel pipe, polymer-coated steel pipe, or composite posts; and shall conform to the specifications for the same material under paragraph 162-2.3.  The fabric shall be of the same type material as used in the fence.

MATERIAL REQUIREMENTS.  Add the following to this section:

ASTM F 1043 Strength and Protective Coatings on Metal Industrial Chain Link Fence Framework

ASTM G 23 -- Operating Light-Exposure Apparatus (Carbon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

ASTM G 26 -- Operating Light-Exposure Apparatus (Xenon-Arc Type) With and Without Water for

Exposure of Nonmetallic Materials

ASTM G 53 -- Operating Light- and Water-Exposure Apparatus (Fluorescent UV-Condensation Type)

for Exposure of Nonmetallic Materials