SUPPLEMENTAL SPECIFICATION NO. 6

P-625, Coal Tar Sealcoat

This Supplemental Specification amends the provisions of the Standard Specifications for Airport Construction, 1998 Edition, and shall be considered to be a part of those Standard Specifications, superseding any conflicting provisions in the Standard Specifications applicable to work under the Contract.

625–3.2  JOB MIX FORMULA.  Delete Table 2 from this subsection and insert the following in its place:

| Type | Coat | Composition and Quantities |
| --- | --- | --- |
|  |  | Water gal./gal. of emul. | Aggregate lbs/gal. of emul. | Rubber gal./gal. of emul. | Application Rate gal./sq.yd. (per application) |
| Heavy Sand Loading | Tack | 3 | – | – | 0.05–0.10 |
|  | Rubberized Sand Slurry | 0.80(max) | 16–20 | 0.10-0.14 | 0.35-0.55 |
|  | Rubberized Emulsion | 0.80(max) | – | 0.03–0.05 | 0.20-0.25 |
| Light Sand Loading | Tack | 3 | – | – | 0.05–0.10 |
|  | Rubberized Sand Slurry | 0.65(max) | 3-8 | 0.03–0.06 | 0.10-0.20 |
|  | Rubberized Emulsion | 0.65(max) | – | 0.03–0.05 | 0.10-0.15 |

625–7.1 BASIS OF PAYMENT. Delete Pay Items from this subsection and insert the following in its place:

Standard Pay Items for Work covered by this Specification are as follows:

| Pay Item P62501 | Rubberized Coal Tar Pitch Emulsion Seal Coat, Heavy Sand Loading, per square yard |
| --- | --- |
| Pay Item P62502 | Rubberized Coal Tar Pitch Emulsion Seal Coat, Light Sand Loading, per square yard |
| Pay Item P62503 | Independent Consultant Services, per day |