# Cleaning and Painting Bearings, Item SPV.0060.XX.

A  Description

This special provision describes cleaning and painting the existing steel bearings on structures as shown on the plans, as directed by the engineer, and in accordance with section 517 of the standard specifications.

B  Materials

Furnish a complete epoxy coating system from the department’s approved product list.  Use the same coating system for all repairs due to handling, shipping and erecting, and for all other uncoated areas.  The color of epoxy shall be white and the urethane coating material shall match the color number shown on the plans in accordance with Federal Standard Number 595B, as printed in 1989. Supply the engineer with the product data sheets before any coating is applied. The product data sheets shall indicate the mixing and thinning directions, the minimum drying time for shop or field applied coats, and the recommended procedures for coating galvanized bolts, nuts, and washers.

C  Construction

C.1  Surface Preparation

Clean areas of loose paint and rust by wire brushing, grinding, or other mechanical means. Sound paint does not need to be removed.

After clean up and storage of waste material, blast cleaning is allowed for only those areas where paint has been removed.  Shield adjacent painted areas during blast cleaning operations.  The blasting sand does not have to be collected.

Furnish adequate containment methods as required to contain and collect waste material resulting from the preparation of painted steel surfaces for painting.  All clean up activities should minimize dust.  Store waste materials in hazardous waste containers provided by the department.

C.2  Coating Application

Apply paint in a neat, workmanlike manner, and in accordance with the manufacturer’s instructions and recommendations. Paint application shall be brushed on.

D  Measurement

The department will measure Cleaning and Painting Bearings as each individual bearing acceptably completed.

E  Payment

The department will pay for the measured quantity at the contract unit price under the following bid item:

| ITEM NUMBER | DESCRIPTION | UNIT |
| --- | --- | --- |
| SPV.0060.xx | Cleaning and Painting Bearings | Each |

Payment is full compensation for preparing and cleaning the designated bearings; furnishing and applying the paint; cleaning up, and containing and collecting all waste materials; and for furnishing all labor, tools, equipment, materials, and incidentals necessary to complete the contract work.

07/05