# Concrete Masonry Bridges Lightweight, Item SPV.0035.XX.

A  Description

This special provision describes furnishing and placing lightweight concrete masonry for the open grid bridge deck in accordance with section 502 of the standard specifications, as shown on the plans, and as hereinafter provided.

B  Materials

This work requires that the open-grid deck be filled with lightweight concrete masonry having a maximum plastic unit weight of 120 pounds per cubic foot.  The lightweight concrete shall have a compressive strength of 4,000 psi at 28 days.  The contractor is responsible for the lightweight concrete mix design.

C  Construction

To prove the design meets the given criteria, provide the engineer with the mix design and 6 test cylinders cured a minimum of 7 days, at least 4 days prior to the anticipated grid deck pour.

Monitor air content using the volumetric method.

Delay the pour if the temperature within 48 hours following the proposed pour is predicted to fall below 40( F (5( C).

Give the concrete a continuous wet cure for a period of 7 days.

D  Measurement

The department will measure Concrete Masonry Bridges Lightweight by the cubic yard acceptably completed, in accordance with subsection 502.4.2 of the standard specifications.

E  Payment

The department will pay for the measured quantity at the contract unit price under the following bid item:

| ITEM NUMBER | DESCRIPTION | UNIT |
| --- | --- | --- |
| SPV.0035.xx | Concrete Masonry Bridges Lightweight | CY |

Payment shall be in accordance with subsection 502.5.2 of the standard specifications, and includes furnishing all labor, tools, equipment, materials, and incidentals necessary to complete the contract work.

07/05