Parapet Concrete Type ‘TX’, Item SPV.0090.01.

A  Description

This special provision describes construction of a decorative concrete parapet in accordance with section 501, 502, and 505 of the Standard Specifications, as shown on the plans, and as hereinafter provided. The concrete mix used for this parapet shall include polypropylene fibers.

B  Materials

The polypropylene fibers shall be engineered synthetic reinforcing fibers of 100% polypropylene collated fibers.

The physical properties of the fibers shall be as follows:

Specific Gravity:		0.91

Denier:				Less than 100

Modulus of Elasticity:		0.5x106 to 0.7x106 psi

Tensile Strength:		70 to 110 ksi

Length:			1/2 to 2-1/2 inches

The polypropylene fiber manufacturer shall certify in writing that all polypropylene fibers are specifically manufactured for use in concrete from virgin polypropylene and the physical properties are within the limits specified above.

If the fiber manufacturer is other than the brand name listed on the literature and/or packaging, the certification must be from the original manufacturer of the polypropylene fibers.

The fiber length shall be determined by the manufacturer to be compatible with the concrete mix design.

C  Construction

The polypropylene fiber manufacturer or authorized distributor shall provide the services of a qualified engineer or employee for a pre-construction meeting and initial job start up.

Use polypropylene fibers at the rate of one bag weighing 1.5 to 1.6 pounds per cubic yard of concrete. The fibers may be added with the fine and coarse aggregates or in the mixer after all ingredients have been blended and mixed in accordance with manufacturer’s recommendations.

D  Measurement

The department will measure Parapet Concrete Type ‘TX’ by the linear foot of parapet acceptably completed.

E  Payment

The department will pay for measured quantities at the contract unit price under the following bid item:

| ITEM NUMBER | DESCRIPTION | UNIT |
| --- | --- | --- |
| SPV.0090.01 | Parapet Concrete Type ‘TX’ | LF |

Payment is full compensation for furnishing all labor, tools, equipment, materials, and incidentals necessary to complete the work.