000-Notes to designer: (DELETE FROM CONTRACT)
1. Flowable Backfill, Item SPV.0035.xx
A  Description
This special provision describes providing and placing flowable backfill as shown in the plans.
B  Materials
Furnish backfill material consisting of aggregates that conform to standard spec 501 for Grade A concrete and do not add any cementitious material; cement or fly ash, to the flowable fill mix. Weigh aggregates at a batch plant suitable for batching concrete masonry. Mix and deliver to the project site using a truck mixer. Add enough water to enable the mixture to flow readily. Submit a mix design, including material source and quantity, to the engineer 14 calendar days before use.
C  Construction
Fill all voids behind timber lagging and excavated soil with flowable backfill. Prior to placement of flowable backfill, provide for positive drainage of the area to be backfilled. Discharge from the truck in a manner to prevent segregation. Completely fill excavation in a single operation. Consolidation or compaction effort is not required.
D  Measurement
The department will measure Flowable Backfill by the cubic yard, acceptably completed.
E  Payment
The department will pay for measured quantities at the contract unit price under the following bid item:
ITEM NUMBER	DESCRIPTION	UNIT
SPV.0035.xx.	Flowable Backfill	CY
Payment is full compensation for providing and placing flowable backfill.
SPV.0035.xx (20260714)
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